Title:

Electro-oxidation of ethanol and its intermediate products: a two-step sequence of efficient PtSn@Rh/C synthesis

Authors & affiliations:

S.Song1, Ch.He1, J.Liu1, Y.Wang2, A.Brouzgou3, F.Tzorbatzoglou3, P.Tsiakaras3, * 1 State Key Laboratory of Optoelectronic Materials and Technologies, School of Physics and Engineering, Sun Yat-sen University, China 2 School of Chemistry and Chemical Engineering, Sun Yat-sen University, China. 3 Department of Mechanical Engineering, School of Engineering, University of Thessaly, Greece. * e-mail: tsiak@uth.gr

Abstract: (Your abstract must use Normal style and must fit in this box. Your abstract should be no longer than 300 words. The box will ‘expand’ over 2 pages as you add text/diagrams into it.)

A two step sequence process has been adopted for PtSn@Rh/C-HT (heat treated) synthesis. Rhodium has been firstly deposited on the carbon support and then PtSn, through microwave assisted polyol method, followed by heat treatment in a reductive atmosphere. It was found that this well-designed process provided PtSn@Rh/C-HT catalyst with a more negative onset potential and high current values towards the electro-oxidation of ethanol as well as its intermediate products. Moreover, the heat-treated PtSn@Rh/C exhibited significantly enhanced activity towards the electro-oxidation of ethanol as well as its oxidation intermediate products (acetaldehyde and acetic acid) compared to the untreated PtSn@Rh/C and PtSnRh/C by the one-step method. The heat-treated PtSn@Rh/C showed quite different behavior especially for acetic acid electro-oxidation, with the disappearance of characteristic peaks for hydrogen adsorption-desorption but with significant oxidation current of acetic acid. This suggests the C-C bond cleavage occurred over the heat-treated PtSn@Rh/C. The present research work describes a promising catalyst preparation method for optimizing Pt-Sn-Rh ternary catalysts for oxidizing ethanol with high activity and high selectivity towards CO2. Keywords:PtSn@Rh/C, ethanol electrooxidation, acetaldehyde electrooxidation, acetic acid electro-oxidation